| OP. NUMBER | Description | Times | Actual Data |
| --- | --- | --- | --- |
| 1 | Reactor 002-XX preparation: 1. Hold Reactor at temperature for 15min. 2. Set Argon flow during heating to 10-15 L/min. 3. Set Argon flow during cooling to 1-2 L/min. COMMENT INFO: FOR REACTOR CHECK AND BLADE CHECK. | Start: __:__ End: __:__ |  |
| 2 | 1. Weigh Materials: 2. Prepare Suspension: c. Ensure that the suspension is well mixed. 3. Load Suspension into Reactor: a. Set/Adjust temperature on thermostat 011-XX to 20oC (keep jacket/RM temp. difference below 50oC). b. Keep the temperature of reaction mixture in range: 15-25oC. d. Load the suspension into Reactor by carefully pouring through a funnel "TP.2 ATI" trying to minimize splashing and exposure. 4. Stirring: a. Set the stirring speed to 150-200rpm (recommended range) (range is recommended and can be adjusted). b. Note: Ensure stirring is adequate to keep the suspension homogeneous. Record required parameters into table XX every YY min. ......................... (eg. XXXX-XXX) ......................... (eg. XXXX-XXX) COMMENT INFO: very dusty product. 4kg per 150L reactor is limiting. Use Acetone for susp. The dusty product before loading. in sop we can describe how to initiate stirring in case if it stopped. Stopping stirrer during reaction itself is not critical as long as we can resume stirring | Start: __:__ End: __:__ | Actual temperature set : ........ oC; Actual temperature: ........ oC; Actual stirring set: ........ rpm; |
| 3 | Load Acetone into reactor 002-XX: 1. Weigh Acetone on balance 007-XX 2. Transfer Acetone into reactor with peristaltic pump and hose "TP.2 ATI". Set peristaltic pump to 50-90%. 3. Set/Adjust stirring rate in reactor to 190-210rpm (range is recommended and can be adjusted). 4. Set/Adjust inert gas flow rate to 1-2 L/min. 5. Set/Adjust temperature on heating/cooling circulator 011-XX to 20oC (keep jacket/RM temp. difference below 50oC). 6. Keep reaction mixture temperature in range: 15-25oC. 7. Addition speed - in one portion. 8. Keep/Provide temperature of loaded material in range: 15-25oC (not controlled). Fill Table X at least every Y minutes. Specified loading: ….. kg (range: … - … kg) COMMENT INFO: Can we have use different blade for stiring shaft? The stirring must be at max, because a lot of solid Ka2CO3 needs to be suspended. | Start: __:__ End: __:__ | Warehouse code: ............ (e.g. XXXX-XX) 1 ......... kg 2 ......... kg 3 ......... kg 4 ......... kg Total ......... kg Actual peristaltic pump set: ........ %; Actual stirring set: ........ rpm; Actual gas flow set: ........ L/min; Actual temperature set : ........ oC; |
| 4 | Load Potassium carbonate into reactor 002-XX: 1. Remove secondary package and open primary package. 2. Weigh Potassium carbonate on balance 007-XX into jug "TP.2 ATI". 3. Load Potassium carbonate into reactor via handhole using a plastic scoop and plastic funnel "TP.2 ATI". 4. Set/Adjust stirring rate in reactor to 190-210rpm (range is recommended and can be adjusted). 5. Set/Adjust inert gas flow rate to 1-2 L/min. 6. Set/Adjust temperature on heating/cooling circulator 011-XX to 20oC (keep jacket/RM temp. difference below 50oC). 7. Keep reaction mixture temperature in range: 15-25oC. 8. Addition speed - portionwise. 9. Keep/Provide temperature of loaded material in range: 15-25oC (not controlled). Fill Table X at least every Y minutes. Specified loading: ….. kg (range: … - … kg) COMMENT INFO: 100L volume - this is probably max scale for 150L glass reactor with propeller blades. Check if we can reduce amount of k2co3??? Check dev report. Was tested. Can't be reduced critical to not stop stirring. Problems resuming stirring ADD VISUAL CHECK OF EFFICIENCY OF STIRRING. EMPHASICE HOW IMPORTANT IT IS | Start: __:__ End: __:__ | Warehouse code: ............ (e.g. XXXX-XX) 1 ......... kg 2 ......... kg 3 ......... kg 4 ......... kg Total ......... kg Actual stirring set: ........ rpm; Actual gas flow set: ........ L/min; Actual temperature set : ........ oC; |
| 5 | Start a hold time: 1. Set/Adjust heating/cooling circulator 011-XX to 20oC. 2. Keep reaction mixture temperature in range: 15-25oC for 30-60min. 3. Set/Adjust stirring in reactor 002-XX to 190-210rpm (range is recommended and can be adjusted). 4. Set/Adjust inert gas flow rate to 1-2 L/min. Fill Table X at least every Y minutes. | Start: __:__ End: __:__ | Actual temperature set : ........ oC; Actual temperature: ........ oC; Actual stirring set: ........ rpm; Actual gas flow set: ........ L/min; |
| 6 | Load Iodoethane into reactor 002-XX: 1. Weigh Iodoethane on balance 007-XX 2. Transfer Iodoethane into reactor with peristaltic pump and hose "TP.2 ATI". Set peristaltic pump to 50-80%. 3. Set/Adjust stirring rate in reactor to 190-210rpm (range is recommended and can be adjusted). 4. Set/Adjust inert gas flow rate to 1-2 L/min. 5. Set/Adjust temperature on heating/cooling circulator 011-XX to 20oC (keep jacket/RM temp. difference below 50oC). 6. Keep reaction mixture temperature in range: 15-25oC. 7. Addition speed - one portion. 8. Keep/Provide temperature of loaded material in range: 15-25oC (not controlled). Fill Table X at least every Y minutes. Specified loading: ….. kg (range: … - … kg) COMMENT INFO: no exotherm is expected here. Toxic wear mask. | Start: __:__ End: __:__ | Warehouse code: ............ (e.g. XXXX-XX) 1 ......... kg 2 ......... kg 3 ......... kg 4 ......... kg Total ......... kg Actual peristaltic pump set: ........ %; Actual stirring set: ........ rpm; Actual gas flow set: ........ L/min; Actual temperature set : ........ oC; |
| 7 | Start heating/cooling with heating/cooling circulator 011-XX: 1. Check that cooling water for 011-XX is opened. 2. Set/Adjust temperature on 011-XX to 75 ->67-63oC (keep jacket/RM temp. difference below 50oC). 3. Keep reaction mixture temperature in range: 52-56oC. 4. Provide temperature gradient: straight. 5. Set/Adjust stirring in reactor 002-XX to 190-210rpm (up to max) should be very effeciently (range is recommended and can be adjusted). Fill Table X at least every Y minutes. COMMENT INFO: turn off the argon IO suggested to keep it sub-boiling. Maxim said no. Can be tested. Yes. Keep it sub boiling keeping in mind 50oC delta between the jacket temp. and rm temp set up cold trap on the exit of reactor to catch iodoethan during pre-val we tested sub-boiling for only 1 day instead of 2 and even though IPC was ok (no SM), the yield was low (almost 8% lower than expected) and it is belived the reason is too short Reaction Time. Reaction should go for 2 days. in validation one sub batch subboiling in 2 days reaction and second boiling and 2 days | Start: __:__ End: __:__ | Actual temperature set : ........ oC; Actual temperature: ........ oC; Actual stirring set: ........ rpm; |
| 8 | Start a hold time: 1. Set/Adjust heating/cooling circulator 011-XX to 67-63oC. 2. Keep reaction mixture temperature in range: 52-56oC for 44-72h. 3. Set/Adjust stirring in reactor 002-XX to 190-210rpm (up to max) should be very effeciently (range is recommended and can be adjusted). 3. Optional: Possible pause - Keep for at least 2 days. Fill Table X at least every Y minutes. COMMENT INFO: 1st day rm is dark red. 3rd day it is dark orange susp. A large deposit of carbonate on the bottom was present whole time in 3kg tech batch we kept it for overweekend NLT 44h reaction time | Start: __:__ End: __:__ | Actual temperature set : ........ oC; Actual temperature: ........ oC; Actual stirring set: ........ rpm; |
| 9 | In-process control: In-process control (determination of IP.X conversion after 44h): 1. Take approximately 1mL of reaction mixture into a 20 mL vial; 2. Purge the vial with argon; 3. Label the sample with an IPC number. For example: TBD-0XXX-Y IP.X RM IPC 1, where Y is the batch number (copied from the header) and X is the IPC serial number. 4. Submit the sample to QC for analysis. 5. Keep stirring the reaction mixture until the IPC result is available. 6. Estimated time for analysis: 1-2h Decision criteria based on IPC result: • If IP.X conversion is conv. 99%; [WARNING, PARAMETER IS CY], proceed with the workup (Operation XX). • On IPC failure: continue boiling, no need to add anything. • On IPC pass: continue next op. IPC 1: TBD-0XXX-Y IP.X RM IPC 1 Results: Corresponds to RelS requirements:  - Yes  - No IP.X conversion: ..... % COMMENT INFO: for pre-val we can take more ipcs to see the progress. think how to take ipc without cooling the reactor. Sample of suspension should be taken now, we need to decide about those possible interm. That we need to control in IPC as well? take sample at ~24h for validation | Start: __:__ End: __:__ | Result: ..............; |
| 10 | Start heating/cooling with heating/cooling circulator 011-XX: 1. Check that cooling water for 011-XX is opened. 2. Set/Adjust temperature on 011-XX to 20->0oC -> 20oC (keep jacket/RM temp. difference below 50oC). 3. Keep reaction mixture temperature in range: 15-25oC. 4. Provide temperature gradient: can be set 20oC overnight. 5. Set/Adjust stirring in reactor 002-XX to 190-210rpm (range is recommended and can be adjusted). Fill Table X at least every Y minutes. COMMENT INFO: keeping in mind 50oC delta between the jacket temp. and rm temp | Start: __:__ End: __:__ | Actual temperature set : ........ oC; Actual temperature: ........ oC; Actual stirring set: ........ rpm; |
| 11 | Start a hold time: 1. Set/Adjust heating/cooling circulator 011-XX to 20oC. 2. Keep reaction mixture temperature in range: 15-25oC for 1-2h. 3. Set/Adjust stirring in reactor 002-XX to OFF (range is recommended and can be adjusted). 4. Optional: Possible pause - can be kept overnight. Fill Table X at least every Y minutes. COMMENT INFO: 1st day rm is dark red. 3rd day it is dark orange susp. A large deposit of carbonate on the bottom was present whole time in 3kg tech batch we kept it for overweekend NLT 44h reaction time | Start: __:__ End: __:__ | Actual temperature set : ........ oC; Actual temperature: ........ oC; Actual stirring set: ........ rpm; |
| 12 | Decant liquid part from reactor 002-XX: 1. Set/Adjust heating/cooling circulator 011-XX to 20oC. 2. Keep reaction mixture temperature in range: 15-25oC. 3. After required time passed, pump liquid part (top layer) from reactor into “direction”. Use peristaltic pump and hose TP.2 ATI. Peristaltic pump set: 50-90%. 4. Stop when pull liquid up to solid part on the bottom. COMMENT INFO: after rm is settled, pull it from top of reactor into container to store product solution. Some light inorganic precipitate can go into product, not a problem, will be washed out later on. | Start: __:__ End: __:__ | Actual temperature set : ........ oC; Actual temperature: ........ oC; Actual peristaltic pump set: ........ %; |
| 13 | Load Water into reactor 002-XX: 1. Weigh Water on balance 007-XX 2. Transfer Water into reactor with peristaltic pump and hose "TP.2 ATI". Set peristaltic pump to 50-90%. 3. Set/Adjust stirring rate in reactor to OFF (range is recommended and can be adjusted). 4. Set/Adjust temperature on heating/cooling circulator 011-XX to 40oC (keep jacket/RM temp. difference below 50oC). 5. Keep reaction mixture temperature in range: 25-35oC. 6. Addition speed - in one portion. 7. Keep/Provide temperature of loaded material in range: 15-25oC (not controlled). Fill Table X at least every Y minutes. Specified loading: ….. kg (range: … - … kg) COMMENT INFO: unblocking stirrer shaft is done manually at first. Start with low rpms, like 15-20rpm at first. | Start: __:__ End: __:__ | Warehouse code: ............ (e.g. XXXX-XX) 1 ......... kg 2 ......... kg 3 ......... kg 4 ......... kg Total ......... kg Actual peristaltic pump set: ........ %; Actual stirring set: ........ rpm; Actual temperature set : ........ oC; |
| 14 | Start a hold time: 1. Set/Adjust heating/cooling circulator 011-XX to 40oC. 2. Keep reaction mixture temperature in range: 25-35oC for 30-50min. 3. Set/Adjust stirring in reactor 002-XX to OFF->15->70rpm. (range is recommended and can be adjusted). Fill Table X at least every Y minutes. COMMENT INFO: 1st day rm is dark red. 3rd day it is dark orange susp. A large deposit of carbonate on the bottom was present whole time in 3kg tech batch we kept it for overweekend NLT 44h reaction time | Start: __:__ End: __:__ | Actual temperature set : ........ oC; Actual temperature: ........ oC; Actual stirring set: ........ rpm; |
| 15 | Perform extraction/separation: 1. Set/Adjust stirring in reactor to OFF (recommended range) (range is recommended and can be adjusted). 2. Mix layers for 30-50min. 3. Stop stirring and let layers completely separate (visual check). Expected time of separation visual check with flashlight. 4. Perform phase separation. Bottom "description" phase is stored into canister "TP.2 ATI", top "description" layer is stored in canister "TP.2 ATI"; At the end layers clearly separated: Yes  / No  (in case of No, inform PM) COMMENT INFO: use flashlight to see phase separation, both layers are dark. Use plastic container to store product while reactor is cleaned | Start: __:__ End: __:__ | Actual stirring set: ........ rpm; Actual separation time: ........ min; |
| 16 | Clean the equipment: 1. Follow the solvent sequence: Water, Acetone. 2. Estimated time required: 0.5h. | Start: __:__ End: __:__ |  |
| 17 | Start evaporation in reactor 002-XX: 1. Set/Adjust temperature heating/cooling circulator 011-XX to 75oC (during pre-val we tested 75) with target 20-62oC (keep jacket/RM temp. difference below 50oC). 2. Connect a membrane pump via a cold trap and turn it ON. 3. Gradually reduce pressure 400->100Torr. Make sure the condenser is not overflooded with condensed solvent, adjust pressure accordingly. 4. Set/Adjust stirring to 150-200rpm (range is recommended and can be adjusted). 5. Continue until: 90-103% from loaded Acetone. 6. Optional: Possible pause - keep overnight, break vacuum, set heating to 20oC and stirring 50rpm.. Fill Table X at least every Y minutes. COMMENT INFO: adjust pressure as needed to avoid overflooding the condenser with solvent "we need to remove iodoethan as much as possible. So there should be really no dripping into cold trap." this is toxic waste | Start: __:__ End: __:__ | Actual temperature set : ........ oC; Actual temperature: ........ oC; Actual pressure: ........ Torr; Actual stirring set: ........ rpm; |
| 18 | Load Anhydrous EtOH into reactor 002-XX: 1. Weigh Anhydrous EtOH on balance 007-XX 2. Transfer Anhydrous EtOH into reactor with peristaltic pump and hose "TP.2 ATI". Set peristaltic pump to use vacuum in reactor. 3. Set/Adjust stirring rate in reactor to 150-200rpm (range is recommended and can be adjusted). 4. Set/Adjust temperature on heating/cooling circulator 011-XX to 35oC (keep jacket/RM temp. difference below 50oC). 5. Keep reaction mixture temperature in range: 20-55oC. 6. Addition speed - one portion. 7. Keep/Provide temperature of loaded material in range: 15-25oC (not controlled). Fill Table X at least every Y minutes. Specified loading: ….. kg (range: … - … kg) COMMENT INFO: set jacket to 35oC and wait until walls are at least 45oC before pulling solvent into reactor with vacuum. | Start: __:__ End: __:__ | Warehouse code: ............ (e.g. XXXX-XX) 1 ......... kg 2 ......... kg 3 ......... kg 4 ......... kg Total ......... kg Actual peristaltic pump set: ........ %; Actual stirring set: ........ rpm; Actual temperature set : ........ oC; |
| 19 | Start evaporation in reactor 002-XX: 1. Set/Adjust temperature heating/cooling circulator 011-XX to 75oC with target 20-62oC (keep jacket/RM temp. difference below 50oC). 2. Connect a membrane pump via a cold trap and turn it ON. 3. Gradually reduce pressure 300->120Torr. Make sure the condenser is not overflooded with condensed solvent, adjust pressure accordingly. 4. Set/Adjust stirring to 150-200rpm (range is recommended and can be adjusted). 5. Continue until: 70-90% from loaded EtOH. 6. Optional: Possible pause - keep overnight, break vacuum, set heating to 20oC and stirring 50rpm.. Fill Table X at least every Y minutes. COMMENT INFO: adjust pressure as needed to avoid overflooding the condenser with solvent "we need to remove iodoethan as much as possible. So there should be really no dripping into cold trap." | Start: __:__ End: __:__ | Actual temperature set : ........ oC; Actual temperature: ........ oC; Actual pressure: ........ Torr; Actual stirring set: ........ rpm; |
| 20 | Start heating/cooling with heating/cooling circulator 011-XX: 1. Check that cooling water for 011-XX is opened. 2. Set/Adjust temperature on 011-XX to 45oC (keep jacket/RM temp. difference below 50oC). 3. Keep reaction mixture temperature in range: 20-62oC. 4. Provide temperature gradient: straight. 5. Set/Adjust stirring in reactor 002-XX to 150-200rpm (range is recommended and can be adjusted). Fill Table X at least every Y minutes. | Start: __:__ End: __:__ | Actual temperature set : ........ oC; Actual temperature: ........ oC; Actual stirring set: ........ rpm; |
| 21 | Load Anhydrous EtOH into reactor 002-XX: 1. Weigh Anhydrous EtOH on balance 007-XX 2. Transfer Anhydrous EtOH into reactor with peristaltic pump and hose "TP.2 ATI". Set peristaltic pump to 50-90%. 3. Set/Adjust stirring rate in reactor to 150-200rpm (range is recommended and can be adjusted). 4. Set/Adjust temperature on heating/cooling circulator 011-XX to 45oC (keep jacket/RM temp. difference below 50oC). 5. Keep reaction mixture temperature in range: 20-62oC. 6. Addition speed - one portion. 7. Keep/Provide temperature of loaded material in range: 15-25oC (not controlled). Fill Table X at least every Y minutes. Specified loading: ….. kg (range: … - … kg) COMMENT INFO: can be added at current temp but then start cooling. | Start: __:__ End: __:__ | Warehouse code: ............ (e.g. XXXX-XX) 1 ......... kg 2 ......... kg 3 ......... kg 4 ......... kg Total ......... kg Actual peristaltic pump set: ........ %; Actual stirring set: ........ rpm; Actual temperature set : ........ oC; |
| 22 | Start heating/cooling with heating/cooling circulator 011-XX: 1. Check that cooling water for 011-XX is opened. 2. Set/Adjust temperature on 011-XX to -10oC->5oC (keep jacket/RM temp. difference below 50oC). 3. Keep reaction mixture temperature in range: 5-10oC. 4. Provide temperature gradient: straight. 5. Set/Adjust stirring in reactor 002-XX to 150-200rpm (range is recommended and can be adjusted). Fill Table X at least every Y minutes. | Start: __:__ End: __:__ | Actual temperature set : ........ oC; Actual temperature: ........ oC; Actual stirring set: ........ rpm; |
| 23 | Start a hold time: 1. Set/Adjust heating/cooling circulator 011-XX to 5oC. 2. Keep reaction mixture temperature in range: 5-15oC for NLT50min. 3. Set/Adjust stirring in reactor 002-XX to 150-200rpm (range is recommended and can be adjusted). 4. Optional: Possible pause - keep overnight. Fill Table X at least every Y minutes. | Start: __:__ End: __:__ | Actual temperature set : ........ oC; Actual temperature: ........ oC; Actual stirring set: ........ rpm; |
| 24 | Filter 046-6-7 setup: 1. Place a PTFE seal on filtrate receiver top edge. 2. Connect suspension receiver to filtrate receiver 3. Install filter cloth into filter and fix it with the plastic ring. 4. Connect hose "TP.2 ATI" to filtrate receiver vacuum valve. Connect other end of hose to a membrane pump 001-XX. Membrane pump 001-XX connected to receiver vacuum valve:  Filtration cloth is cut and installed properly:  Filter 046-2-13 setup: 5. Connect suspension receiver to glass receiver from reactor 002-XX with norprene hose "TP.2 ATI". 6. Connect reactor receiver to membrane pump 001-XX with norprene hose "vacuum". 7. Install filter cloth into filter and fix it with the plastic ring. Filter is connected to Reactor's receiver vessel:  Membrane pump 001-XX is connected to Reactor's receiver vacuum valve:  Filtration cloth is cut and installed properly:  | Start: __:__ End: __:__ |  |
| 25 | Filter the material: 1. Keep stirring in Reactor 002-XX to 150-60rpm (gradually decreasing). 2. Connect norprene hose "TP.2 ATI" from reactor valve and through peristaltic pump 001-XX to Nutsch filter. Set the peristaltic pump to 40-60%. 3. Set the vacuum pump to 300Torr and start it. 4. Start peristaltic pump, open reactor’s valve and transfer the reaction mixture from the Reactor to the Nutsch filter in portions, allowing filtration to proceed. 5. Continue until: until Filter Cake is dry. 6. Use a spoon "TP.2 ATI" to press and remove cracks that might appear on filter cake. NB! Once Reactor’s receiver is 2/3 full, stop the process, release the vacuum from the system, connect filter outlet to atmosphere and empty filtrate into "TP.2 ATI". Resume the process afterwards. COMMENT INFO: not air/water sensitive use filter 046-13 and reactor's receiver as f-bottle use plastic filter here add everywhere toxic open handling with care (before it washed on the filter.) | Start: __:__ End: __:__ | Actual set: ........ Torr; |
| 26 | Wash filter cake with Anhydrous EtOH: 1. Stop membrane pump 001-XX. Connect outlet to the atmosphere (to prevent filter cloth from floating). 2. Use Anhydrous EtOH for washing Filter cake 3. Ensure loaded material temperature is 15-25oC (not controlled). 4. Mix on filter: manual mixing on filter. 5. Restart membrane pump and continue filtration. Specified loading: ….. kg (range: … - … kg) COMMENT INFO: use minimal amount of EtOH to first wash Filter Cake, this improves furthere washing with water significantly | Start: __:__ End: __:__ | Warehouse code: ............ (e.g. XXXX-XX) 1 ......... kg 2 ......... kg 3 ......... kg 4 ......... kg Total ......... kg |
| 27 | Filter the material: 1. Keep stirring in Reactor 002-XX to 150-60rpm (gradually decreasing). 2. Connect norprene hose "TP.2 ATI" from reactor valve and through peristaltic pump 001-XX to Nutsch filter. Set the peristaltic pump to 40-60%. 3. Set the vacuum pump to 300Torr and start it. 4. Start peristaltic pump, open reactor’s valve and transfer the reaction mixture from the Reactor to the Nutsch filter in portions, allowing filtration to proceed. 5. Continue until: until Filter Cake is dry. 6. Use a spoon "TP.2 ATI" to press and remove cracks that might appear on filter cake. NB! Once Reactor’s receiver is 2/3 full, stop the process, release the vacuum from the system, connect filter outlet to atmosphere and empty filtrate into "TP.2 ATI". Resume the process afterwards. COMMENT INFO: not air/water sensitive | Start: __:__ End: __:__ | Actual set: ........ Torr; |
| 28 | Wash filter cake with Water: 1. Stop membrane pump 001-XX. Connect outlet to the atmosphere (to prevent filter cloth from floating). 2. Use Water for washing Filter cake 3. Ensure loaded material temperature is 15-25oC (not controlled). 4. Mix on filter: manual mixing on filter. 5. Restart membrane pump and continue filtration. Specified loading: ….. kg (range: … - … kg) COMMENT INFO: product contains ca 60% of inorganic soluble in water. | Start: __:__ End: __:__ | Warehouse code: ............ (e.g. XXXX-XX) 1 ......... kg 2 ......... kg 3 ......... kg 4 ......... kg Total ......... kg |
| 29 | Filter the material: 1. Keep stirring in Reactor 002-XX to 150-60rpm (gradually decreasing). 2. Connect norprene hose "TP.2 ATI" from reactor valve and through peristaltic pump 001-XX to Nutsch filter. Set the peristaltic pump to 40-60%. 3. Set the vacuum pump to 300Torr and start it. 4. Start peristaltic pump, open reactor’s valve and transfer the reaction mixture from the Reactor to the Nutsch filter in portions, allowing filtration to proceed. 5. Continue until: until Filter Cake is dry. 6. Use a spoon "TP.2 ATI" to press and remove cracks that might appear on filter cake. NB! Once Reactor’s receiver is 2/3 full, stop the process, release the vacuum from the system, connect filter outlet to atmosphere and empty filtrate into "TP.2 ATI". Resume the process afterwards. COMMENT INFO: volume of F cake after firt water wash will be reduced. This is normal | Start: __:__ End: __:__ | Actual set: ........ Torr; |
| 30 | Wash filter cake with Water: 1. Stop membrane pump 001-XX. Connect outlet to the atmosphere (to prevent filter cloth from floating). 2. Use Water for washing Filter cake 3. Ensure loaded material temperature is 15-25oC (not controlled). 4. Mix on filter: manual mixing on filter. 5. Restart membrane pump and continue filtration. Specified loading: ….. kg (range: … - … kg) | Start: __:__ End: __:__ | Warehouse code: ............ (e.g. XXXX-XX) 1 ......... kg 2 ......... kg 3 ......... kg 4 ......... kg Total ......... kg |
| 31 | Filter the material: 1. Keep stirring in Reactor 002-XX to 150-60rpm (gradually decreasing). 2. Connect norprene hose "TP.2 ATI" from reactor valve and through peristaltic pump 001-XX to Nutsch filter. Set the peristaltic pump to 40-60%. 3. Set the vacuum pump to 300Torr and start it. 4. Start peristaltic pump, open reactor’s valve and transfer the reaction mixture from the Reactor to the Nutsch filter in portions, allowing filtration to proceed. 5. Continue until: until Filter Cake is dry. 6. Use a spoon "TP.2 ATI" to press and remove cracks that might appear on filter cake. NB! Once Reactor’s receiver is 2/3 full, stop the process, release the vacuum from the system, connect filter outlet to atmosphere and empty filtrate into "TP.2 ATI". Resume the process afterwards. | Start: __:__ End: __:__ | Actual set: ........ Torr; |
| 32 | Wash filter cake with Water: 1. Stop membrane pump 001-XX. Connect outlet to the atmosphere (to prevent filter cloth from floating). 2. Use Water for washing Filter cake 3. Ensure loaded material temperature is 15-25oC (not controlled). 4. Mix on filter: manual mixing on filter. 5. Restart membrane pump and continue filtration. Specified loading: ….. kg (range: … - … kg) | Start: __:__ End: __:__ | Warehouse code: ............ (e.g. XXXX-XX) 1 ......... kg 2 ......... kg 3 ......... kg 4 ......... kg Total ......... kg |
| 33 | Filter the material: 1. Keep stirring in Reactor 002-XX to 150-60rpm (gradually decreasing). 2. Connect norprene hose "TP.2 ATI" from reactor valve and through peristaltic pump 001-XX to Nutsch filter. Set the peristaltic pump to 40-60%. 3. Set the vacuum pump to 300Torr and start it. 4. Start peristaltic pump, open reactor’s valve and transfer the reaction mixture from the Reactor to the Nutsch filter in portions, allowing filtration to proceed. 5. Continue until: until Filter Cake is dry. 6. Use a spoon "TP.2 ATI" to press and remove cracks that might appear on filter cake. NB! Once Reactor’s receiver is 2/3 full, stop the process, release the vacuum from the system, connect filter outlet to atmosphere and empty filtrate into "TP.2 ATI". Resume the process afterwards. | Start: __:__ End: __:__ | Actual set: ........ Torr; |
| 34 | Wash filter cake with Anhydrous EtOH: 1. Stop membrane pump 001-XX. Connect outlet to the atmosphere (to prevent filter cloth from floating). 2. Use Anhydrous EtOH for washing Filter cake 3. Ensure loaded material temperature is 15-25oC (not controlled). 4. Mix on filter: manual mixing on filter. 5. Restart membrane pump and continue filtration. Specified loading: ….. kg (range: … - … kg) COMMENT INFO: product remained grey | Start: __:__ End: __:__ | Warehouse code: ............ (e.g. XXXX-XX) 1 ......... kg 2 ......... kg 3 ......... kg 4 ......... kg Total ......... kg |
| 35 | Filter the material: 1. Keep stirring in Reactor 002-XX to 150-60rpm (gradually decreasing). 2. Connect norprene hose "TP.2 ATI" from reactor valve and through peristaltic pump 001-XX to Nutsch filter. Set the peristaltic pump to 40-60%. 3. Set the vacuum pump to 300Torr and start it. 4. Start peristaltic pump, open reactor’s valve and transfer the reaction mixture from the Reactor to the Nutsch filter in portions, allowing filtration to proceed. 5. Continue until: until Filter Cake is dry. 6. Use a spoon "TP.2 ATI" to press and remove cracks that might appear on filter cake. NB! Once Reactor’s receiver is 2/3 full, stop the process, release the vacuum from the system, connect filter outlet to atmosphere and empty filtrate into "TP.2 ATI". Resume the process afterwards. | Start: __:__ End: __:__ | Actual set: ........ Torr; |
| 36 | Wash filter cake with Anhydrous EtOH: 1. Stop membrane pump 001-XX. Connect outlet to the atmosphere (to prevent filter cloth from floating). 2. Use Anhydrous EtOH for washing Filter cake 3. Ensure loaded material temperature is 15-25oC (not controlled). 4. Restart membrane pump and continue filtration. Specified loading: ….. kg (range: … - … kg) | Start: __:__ End: __:__ | Warehouse code: ............ (e.g. XXXX-XX) 1 ......... kg 2 ......... kg 3 ......... kg 4 ......... kg Total ......... kg |
| 37 | Filter the material: 1. Keep stirring in Reactor 002-XX to 150-60rpm (gradually decreasing). 2. Connect norprene hose "TP.2 ATI" from reactor valve and through peristaltic pump 001-XX to Nutsch filter. Set the peristaltic pump to 40-60%. 3. Set the vacuum pump to 300Torr and start it. 4. Start peristaltic pump, open reactor’s valve and transfer the reaction mixture from the Reactor to the Nutsch filter in portions, allowing filtration to proceed. 5. Continue until: until Filter Cake is dry. 6. Use a spoon "TP.2 ATI" to press and remove cracks that might appear on filter cake. NB! Once Reactor’s receiver is 2/3 full, stop the process, release the vacuum from the system, connect filter outlet to atmosphere and empty filtrate into "TP.2 ATI". Resume the process afterwards. | Start: __:__ End: __:__ | Actual set: ........ Torr; |
| 38 | Dry the filter cake on filter under vacuum: 1. Once Filter cake is visually dry, maintain it on the filter under vacuum. 2. Continue to apply vacuum 300Torr for 20-30min to remove residual solvents. 3. Use a spoon "TP.2 ATI" to press and remove cracks that might appear on filter cake. 4. Consider air, moisture, and light sensitivity of the material. 5. After finishing drying on filter, pump the filtrate from the filter into waste canister and weigh it. m tara = ....... kg ; m gross weight = ....... kg ; m net "type of waste" waste = ....... kg ; | Start: __:__ End: __:__ | Actual set: ........ Torr; |
| 39 | Dry the product in oven 012-XX: 1. Check and record the tare mass of each tray into table XX.1. 2. Transfer the product (filter cake) onto trays with a layer thickness of NMT 4cm. Divide all wet product approximately evenly between all trays. Crush big lumps with shovel. 3. Place the trays in the oven. 4. Set temperature of the oven to 40-45oC with overheating protection: 55oC. 5. Adjust fan to: set 70%. 6. Set flap to set 70%. 7. Dry the product, checking the weight periodically (NLT 12h after start of drying) to determine dryness 24-48h. 8. Perform Mix/delump: after 12-18h. Record weights in Table X. Table X filled:  Overheating set: .......°C Actual fan set: .......%; Actual flap set: .......%; Temperature after at least 1h from the start: .......°C COMMENT INFO: rnd will conduct test of drying at 50oC; Maksim says 50oC is ok check weigh of trays | Start: __:__ End: __:__ | Actual temperature set : ........ oC; |
| 40 | Finish drying: 1. Save heating/cooling circulator 011-XX temperature logs on the USB stick that is inside the control panel or in the USB ports. 2. Turn off membrane pump and repressurize the oven. Turn off the oven. 3. Remove the trays from the oven and weigh them. Calculate loss on drying and fill Table X. 4. Calculate process yield: | Start: __:__ End: __:__ |  |
| 41 | Pack the product: | Start: __:__ End: __:__ |  |
| 42 | Perform the analysis according to QDQS: 1. If analysis result is YES, proceed accordingly. 2. If analysis result is NO, repeat necessary steps. | Start: __:__ End: __:__ |  |
| 43 | Clean the equipment: | Start: __:__ End: __:__ |  |
| 44 | Perform waste treatment: 1. Process organic waste: can contain ethyliodide. Toxic waste label.. | Start: __:__ End: __:__ |  |